Descriptions of QT10-15 Block Machine:

“QT” in QT 10-15 is given by Chinese government that all of the Concrete Block machine must use this Series Number.

“10” in QT10-15 stands for the production quantity is 10 blocks "390×190×190mm" per mould,

“15” in QT10-15 stands for one cycle time is 15 seconds.

Since the moulds are changeable, the concrete equipment is able to produce different types of blocks/bricks, and this is a hydraulic machine can produces a stronger block, due to the greater pound pressure applied by the hydraulic system.

The block manufacturer can also realize substantial savings by using less cement. A ratio from 8:1 to 11:1 sand/cement can be achieved. This machine is designed for the manufacturer with a steady year turnover and with a certain number casher to make the factory running.

This machines can be equipped with an automatic elevator/skip for loading mix into hopper, agitator, an automatic pallet feeder, pallet ejector, brush for cleaning blocks and a run off conveyor (see above). It is suggested that you use a high capacity mixer of over 500 liters. A work force of 20 to 50 employees would keep this factory running at full capacity.

QT 10-15 Model Specification

| Hollow Block Capacity(390×190×190mm) | 10/module |
| --- | --- |
| Solid Brick Capacity(240×115×53mm) | 54/module |
| Holland Brick Capacity(240×115×90mm) | 27/module |
| Main Dimension(L×W×H) | 8200×2000×2950(mm) |
| Pallet Size(L×W×H) | 1150×840×40(mm) |
| Pressure Rating | 12~25Mpa |
| Vibration | 50~90KN |
| Vibration Frequency | 2900~5600r/min |
| Cycle Time | 15-20(s) |
| Power(Total) | 36kw |
| Weight | 11000kg |
| Hollow Block Capacity(390×190×190mm) | 14400-19200/8hours |
| Solid Brick Capacity(240×115×53mm) | 73440-97920/8hours |
| Holland Brick Capacity(200×100×60mm) | 34560-46086/8hours |

Optional Parts:

1. Skip type concrete mixer……………………. Model JS750

2. Mould:  we can manufacture the a certain special mould for you accordingly .

3. Double layer Color-face device.

Advantages Of QT Series Automatic Block Making Machine:

1. Perfect humanization Electrical control system

Siemens PLC with Visualization touch screen provide you a Child operation machine.

2. Frequency Conversional Control Technology:

It guarantees the precise and parallel movement between tamper head and mould, protects the products from transfiguration; increases the production rate by improving the vibrating efficiency, and Power saving: 30%;

3. Hydraulic System. Make in China, world Quality , and we can provide you the hydraulic motor as you request .

4. Compulsory Feeding system make sure that the density and intensity of the products are guaranteed;

5. Various product scope:

It produces various color-face bricks (layered material feeding),through-body tiles，lock linkage blocks, road curb bricks, hydraulic blocks、hollow blocks, perforated bricks, and standard bricks etc.